RESEARCH ON THE QUALITY OF Cu-Zn-Al SHAPE MEMORY ALLOYS JOINED BY ELECTRIC RESISTANCE POINT - WELDING

Claudia M. Dorohoi1, Ion Mitelea1 & Corneliu M. Crăciunescu2

1”Politehnica” University of Timişoara, Department of Materials and Manufacturing Engineering

2 Universidede Nova de Lisboa, CENIMAT/I3N, Departamento de Ciencia de Materiais

Corresponding author: Dorohoi Claudia – Mariana, dorohoi_claudia@yahoo.com

Abstract: The paper describes the experimental results on welding Cu-Zn-Al shape memory alloys using welding by electric resistance point – joining. The influence of the welding parameters (pressure, current, time) on the resulting microstructural joints is analyzed. Inadequate parameters lead to surface melting and penetrations. Based on macro and microstructural analysis, the optional parameters for joining the Cu-Zn-Al plate’s use in the experiments were 4KA current, 2.2-2.5 bar pressure and 0.06 sec time.

Key words: shape memory alloys, electric resistance point welding, Cu-Zn-Al, microstructure