a railway rail fracture expertises using the electronic microscopy

Munteanu Corneliu1, Pipa George-Radu2, Bărbînţă Constantin-Ioan1, Lorenz Peter3, Chicet Daniela-Lucia1, Bărbînţă Andreea-Carmen1 & Axinte Cătălina1

1Technical University “Gheorghe Asachi” of Iasi-Romania, Department of Machine Design and Mechatronics

2Technical University “Gheorghe Asachi” of Iasi-Romania, Department of Roads and Foundations

3University of Applied Sciences Saarbrücken, Germany

Corresponding author: Bărbînţă Constantin-Ioan, costelbarbinta@yahoo.com

Abstract: In this paper is analysed a rail type 65 which has been exfoliated on a length of about 270 mm. To remove this defect, the exfoliated area has been cleaned by grinding and after that it was realized a covering of the afected area by welding. Finally the rail has been polished to get to the profile from the work drawings, which conditions the its admission in service. After the rail was given back to service, has been fractured, after supporting a traffic of 150.000 tons. To determine the causes of the rail breaking, there were made analyses using modern methods of electronic microscopy. The results show that a particular attention should be given to manufacturing processes, but also to the maintenance and to a suitable diagnosis after possible exfoliation of the rails, to prevent their breaking in service.

Key words: rail, fracture, welding, electronic microscopy.