LUBRICATION REGIMES IN A SPUR GEAR TRANSMISSION

Liviu Balan1, Ana Tufescu2, Dumitru Olaru2

1 Continental Automotive Systems S.R.L., Sibiu-Romania

2Technical University “Gheorghe Asachi” of Iasi-Romania, Dept of Mechanical Engineering, Mechatronics and Robotics

Corresponding author: 	Ana Tufescu, ana.tufescu@yahoo.com

Abstract: The authors have developed a methodology and a computer program to evaluate the lubrication regimes and minimum film thickness in a spur gear transmission. For given geometrical conditions in a lubricated point contact spur gear, was generated the map of lubrication regimes according to the viscosity parameter gv and elasticity parameter ge. The map of lubrication was generated in three contact points on the gear tooth flank: top, pitch and end of the pinion tooth. For given operation conditions (power, rotational speed, lubricant viscosity and temperature) was determined, both the lubrication regime and minimum film thickness. Also the ratio between minimum film thickness and gear teeth flanks roughness has been determined and the risk of scuffing failure was evidenced.

Key words: gear lubrication, map of lubrication, point contact, minimum film thickness, scuffing failure.