Electrochemical discharge machining

of metallic carbide ISO P25

Margareta Coteaţă1, Octavian Lupescu 1, Ovidiu Sava 1, Irina Grigoraş Beşliu2

1Technical University “Gheorghe Asachi” of Iasi-Romania, Department of Machine Manufacturing Technology

Corresponding author: Margareta Coteaţă, mcoteata@tcm.tuiasi.ro

Abstract: Electrochemical discharge machining refers to a machining method based on the developing of electrical discharges simultaneously with an electrochemical dissolution of the workpiece material. The machining method can be applied in the case of the electroconductive materials. The purpose of the research presented in this paper was to characterize the behavior of the metallic carbides during the electrochemical discharge machining process. A factorial experiment was designed and applied by taking into consideration the changing of the tool diameter, of the work gap voltage, of the capacity of the discharge circuit and of the electrolyte density. By mathematical processing of the experimental data, some empirical models were determined.

Key words: electrochemical discharge machining, metallic carbides, factorial experiment, empirical model, drilling