POSITIONING OF THE ELECTROMAGNETIC FORMING PROCESS FOR DRAWING USING COMPARATIVE ANALySiS

Mihai-Cătălin Mocanu-Andrieş 1 , Traian Grămescu1 & Alexandru Rădeanu1

1Technical University “Gheorghe Asachi” of Iasi-Romania, Department of Machine Manufacturing Technology

Mihai-Cătălin Mocanu-Andrieş, madlene_87@yahoo.com

Abstract: This paper work has made a comparative analysis between the place of the electromagnetic process and some processes of drawing of metallic materials. The most representative processes from those that has been analyzed are unconventional and only one is classical. Comparative analysis was developed by underlining the obvious weaknesses and strengths, and the opportunities and threats that can appear within the expanding or restricting of the distribution of such processing methods within the industry. The final result is concentrated under the shape of a die that provides aspects of major importance in developing and maintaining the desired position for the analyzed subject.

Key words: plastic deformation with high speed, electromagnetic field, hydro-forming, electro-hydraulic, SWOT, PEST