INFLUENCE OF WORKING PARAMETERS ON THE DEVIATION FROM CIRCULAR SHAPE OF THE OUTER TOROIDAL SURFACE SUPERPOLISHING

Ionel Sarbu1 & Lucian Tabacaru1

1 “Gheorghe Asachi” University of Iasi

Corresponding author: Ionel Sarbu, sarbu_ionel@yahoo.com

Abstract: In this paper is presented a series of research on superpolishing technology routes running rings groove ball bearings 6203 series in terms of optimizing the choice of bars which afford abrasive surface quality requirements of technical documentation as productivity. Was defined the (AFPCcdr assessment index of deviation from circular shape to superpolishing outer toroidal surface, measurements were made on equipment "ROTARY TALYSURF. They drew diagrams of dependence.

Key words: superpolishing bars, wheels, bearings, radial bearings, quality optimization