THE INFLUENCE OF WORKING PARAMETERS ON THE RESULTS OF THE HEAT TREATMENT APPLIED TO SOME ALUMINUM ALLOYS

Maria Stoicănescu1 & Ana Veţeleanu1

1University “Transilvania” of Braşov, Department of Technological Equipment & Materials Science

Corresponding author: Maria Stoicănescu, E-mail address: stoican.m@unitbv.ro

Abstract: The experimental attempts had as aim, the settlement of optimum heat treatment parameters for some aluminum alloys, like: heating temperature, hardening conditions, ageing technique. The tests were accomplished for three marks of deformabile alloys, which were hardened in water from temperatures between 500(C and 530(C followed by artificial ageing in electromagnetic field.

Key words: aluminium, deformable alloy, heat treatment