INFLUENCE OF DEFORMATION FEED ON THE ROUGHNESS AND SHAPE PRECISION OF COLD WORKED SURFACES

Octavian Pruteanu1, Lucian Tăbăcaru1, Constantin Cărăuşu1 & Traian Grămescu1

1 “Gheorghe Asachi” Technical University of Iasi-Romania, Department of Machine Manufacturing Technology

Corresponding author: Octavian Pruteanu, pluteanu@yahoo.com

Abstract: The paper describes the outcome of our experimental research achieved further to the cold working of the running tracks of two types of radial ball bearings. It tackles the influence of deformation feed on the roughness and shape deviations – out-of-roundness and circularity – suffered by the running tracks. The values thus obtained are shown in the tables and illustrated in the figures, and they ground our conclusions related to the favorable influence intervals.

Key words: plastic deformation, feed, roughness, out-of-roundness, circularity.